	Biosorption of Copper and Lead Ions Using Chara Algae
Salah N. Farhan *1, Walaa Abid Mahmood2, Muataz H. Ismael 3, Anees A. Khadom4, Abdul Mun'em Abbas Karim5

1,2,3,4,5 Diyala University, College of Engineering, Chemical Engineering Departement, Iraq

* Corresponding Author: Email: drsalahchem@gmail.com



Background
A good way to preserve water exceptional requirements which can be appropriate for environmental and human health, elimination of heavy metals from commercial effluents have emerged as very important. Recycling and conservation of crucial metals are becoming increasingly more essential [1]. Human health will be threatened seriously by heavy metal ions via bioconcentration, bioaccumulation, and biomagnifications through a biological chain and drinking water. [2, 3].
As two of classical toxic heavy metals, lead and copper contamination which is derived from wastewater of several industries including plastic and paint manufacturing, mining, petrochemical processes, electroplating, paper and pulp, metallurgical processes, and batteries. Exposure to a higher concentration of copper cause Wilson’s disease which is neurotoxicity, while lead causes anemia, encephalopathy and hepatitis. Ion exchange, chemical precipitation, liquefied lime, reverse osmosis, and electrochemical removal have been used to eliminate heavy metal ions from aqueous solution with significant disadvantages such as cost prohibitive, slurry formation, and high energy requirements. Activated carbon is a very effective method of adsorbing metals but it is limiting due to high cost. Sustainable and effective technology using biologically active or inactive organisms or so-called bio-adsorption (Biosorption) is an emerging way to remove heavy metal ions as its cost is low such as, bamboo dust[4], coconut fiber [5], bagasse [6],  saw dust[7], algae [8], silk cotton hull[9], wheat straw (Triticum sativum)[10],  yeast[11,12]. In water pollution control, biosorption is a very effective way used to eliminate metal ions from containing solutions [13,14]. 

One of the most important advantages of the removal process in this way is the possibility of reusing the adsorbent medium with a low selective cost for the metal ions, even if they are present at low concentrations, as well as the non-generation of toxic substances as an accidental product [15]. The present study is conducted to investigate the efficiency of Chara algae in removal of lead and copper ions (Pb+2 and Cu+2) from prepared solutions. 
 The optimal conditions for the process of bio-adsorption such as pH function, primary metal concentration, contact time, temperature, and quantity of biomaterial are studied. Biosorption mechanisms of Pb+2 and Cu+2 ions onto Chara algae are examined through the kinetics of reactivity and thermodynamics.
Methods
Algae Preparation 
Chara algae used in the present study is obtained from Khuraesan River (Diyala Governorate, Iraq). To remove all the dirt particles, it is washed with tap water and then with distilled water for several times, then left under sunlight for two days for initial drying, then it is placed in an oven at 75 oC for 24 hr to complete the drying process. The dried material is grounded and screened through a set of sieves to get 250 µm, and then stored in a plastic holder before examinations.
Algal ashes Preparation 

Dried algae are heated at 500 ° C for 5 hr for carbonization and then hydrolyzed in 3:1 potassium hydroxide for 2 days. At 80
0 ° C for 3 hrs., calcination is performed to obtain algae ashes [16,17].
Preparation of Synthetic Solution:
Standard solutions of 1g·L-1 of Pb+2 and Cu+2 ions is prepared by dissolving the suitable amount of CuCl2 and Pb(NO3)2 in deionized, distilled water. For the purpose of preventing the deposition of metal ions, drops of hydrochloric acid are added. By dilution with distilled water, working solutions are prepared. Initial pH is controlled via adding HNO3 or NaOH droplets.

FTIR studies of Untreated Chara algae:
Binding mechanism of sorption is explained by FTIR studies, which are carried out to confirm the presence of the functional groups.  Chara algae powder is mixed with KBr of spectral grade and moisture free pellets. The spectrum of FTIR is recorded by Perkin-Elmer spectrum 100, in the range of 450 cm-1 to 4000 cm-1.

Thermal gravimetric analysis (TGA)

Thermal gravimetric analysis is done by a  differential thermal analyzer (ShimadzuDTA-50, Japan) up to 900 °C for both algae and algae ashes. 

Batch mode of Biosorption studies:

To study the effect of acidity, temperature, contact time and primary concentration of metal ions on equilibrium study, batch experiments are conducted at a constant concentration for both of Pb+2, and Cu+2 at 10 mg/L. 50 ml of these ions are placed in conical flasks (250 ml) of known concentration, and biosorbent dose . PHs (2, 3,5, 6 and 8), and a biosorbent dose of  0.1 g/l. for  30 min contact time. The mixture agitated by rotary shaker (DUBNOOT BSD/DCE) for 1 hr at 200 rpm. The pH is controlled by adding 0.1 M NaOH and/or 0.1N HNO3 prior to sorbent addition. After that, centrifugation process is done at 300 rpm for 5 minutes in order to separate supernatants from adsorbent media. Residual metal concentration in supernatants is determined by AAS (Scientific Atomic Absorption Spectrophotometer Accu sys 21), average results is recorded. The biosorption efficiency is measured by the following equation:


[image: image1.wmf])

1

(

100

)

(

0

0

´

-

=

C

C

C

E

e


The following expression is used to predict metal uptake efficiencies of all adsorbents:


[image: image2.wmf](

)

)

2

(

1000

*

0

m

C

C

V

q

e

-

=


Where q represents the amount of metal bonded in mg to 1 g of algae; C0 and Ce  represent initial and final metal concentration( after equilibrium); V refers to the volume of solution in milliliter and m denotes the dry weight of the Chara algae  added.
Biosorption equilibrium

A known amount of Chara algae is put in flasks of volume 250 mL, each flask containing 100 mL of metal ion solution with different initial concentration (20–100 mg/L). These flasks are shaken in a rotary shaker at 2

00 rpm for 1 hr maintaining a temperature at 25 oC . in order to reach saturation condition( biosorbent saturated with metal ions.
 Biosorption kinetics

Kinetics experiments are conducted by using (250) mL flasks containing 100 mL of metal ion prepared solution with specified amount of Chara algae, Flasks are agitated by rotary shaker at 200 rpm with constant temperature at 25 oC, samples collected at various intervals (10-150 min), centrifuged and residual metals in the samples are determined. Pseudo-first and second order models are used to analyzed kinetic results [19,20]. 

Results and Discussion

Identifying the peaks on raw algae

The wall of algal cells is composed of polysaccharides, proteins, and lipids which offer functional groups that is responsible for metal binding [21].  FTIR analysis in the range of 450 cm-1to 4000cm-1, shows the presence of characteristic polymeric –OH as in cases of celluloses and hemicelluloses (Xylan), phenolic –OH as in case of tannins and lignins, O=C-O, carboxylate ion as in glucuronates of a hemi cellulosic present in a bark.

FTIR spectra analysis suggests that the presence of effective groups such as carboxylic and alcohol bonds can be associated with (N-H) amine bond stretching at peaks extended from 3399 to 3434 cm-1; while amide groups or carbonyl C=O bond of within 1080-10920 cm-1; stretchings of alcohol and ethers C-O and O-H bond extended from 1000to 1280 cm-1. At 1400 cm-1 lead could be binding at this site, all these groups are related to individual metal binding. [22].
The FTIR spectra Fig.1 shows that all groups including amino, hydroxyl, carboxylic, and carbonyl groups are exist and have some rules in the adsorption process.
Thermogravimetric Analysis

Thermogravimetric analysis (TGA) for algae and algae ashes as seen in Fig. 2 shows that from 0 to 150 °C, there is loss in mass for samples by up to 20% due to a removal of humidity. Between 300-400 °C, The loss is very high and that could be attributable to decomposition of algae to gases[23]. In algae ashes, there are more hydrophilic groups and its surface area are accepted by activation [24].
Effect of pH:

Chemistry of metals known to be affected by acidic scale, pH of a prepared solution as well as for function group protonation of the functional groups existing on Chara algae surface of.  By increasing the pH, adsorption rate of ions increases to a maximum and then begins to decline sharply. 

As the pH increase, this increases the number of active sites that carry a negative charge on the surface of the absorbent material; the best pH was 6 as shown in figure 3.

Acidic and basic functional groups existing on Chara algae surfaces include the sulfate groups, phosphate, carboxyl, amine, and hydroxyl. In general, sulfate and carboxylic groups are the most effective in the adsorption process [25]. When the acid scale pH is less than 5, the active groups in the cell wall and ionic state are responsible for adsorption and since the metals are present in their ionic form and through acid-acid equilibrium theory, the coupling of metal cations is measured by the dissociation of weak acid groups.

 By using biological materials, carboxylic group (COOH) is most effective in the removing metal ions [26,27]. At pH 5, there are few hydronium ions that compete with heavy metals ions on free bonds at active sites which are negatively charged resulting in an increase in biosorption. An increase of pH in the range of 6-10 causing precipitation process in solution as well as some dip in the polarity. Several adsorbent materials is used to investigate the effect of pH on the adsorption process [28,29]. 

Effect of Temperature:

The increase in temperature increases the prevalence rate of ions during the external boundary layer, internal limits of pores in absorbent material and the best temperature is 40 0C as can be seen in Fig4. Results showed that the process of adsorption is an exothermic process and therefore the increase in temperature slightly lead to decreasing the rate of adsorption. Low temperature is indicative of a physical biosorption phenomenon. 
Bio adsorbent dose 

Using different concentrations of adsorbent material effects on adsorption process as shown in Figure 4. It can be observed that by increasing the amount of adsorbent, the adsorption rate decreases due to the overlapping of active sites.

Effect of contact time

Figure 6 shows that more than 75% of the metal ions are removed in the first 15 minutes and the equilibrium state can be reached after 60 minutes [30]. And then the change in adsorption status is almost unnoticeable.

Using non-living cells is not dependent on the metabolism and occurs at the walls of these cells and the process of adsorption, in this case, is a quick process and more preferred that the case living cells[25].

Initial concentrations effects

 From observation of Fig. 7, the increase in adsorption is directly correlated with the increase of the primary concentration of metal ions. This can be due to the availability of bonding sites for adsorption of abundant ions. The speed of the adsorption process can be observed in the first 15 minutes. Thereafter a decrease in the concentration of ions occurs to the extent of the occupancy of all the active sites and down to the state of equilibrium.

 The speed of the process at first, the first phase, is due to the process of adsorption from the surface of the material obtained by the ion exchange process with the active groups while the second phase is lower and that could be attributed to Interstitial fluxes of metal ions into the cell.          
Conclusions
The current study shows that it is possible to use cheap and available in large quantities, Chara algae, which has the ability to remove toxicity from the outside stream of any industry. The practical results show that the time required for adsorption is short, exothermic nature of a biosorption process, best pH and high affinity for metal ions is found. The use of algae requires more studies on the level of the presence of more than metal and the possibility of finding a mathematical model shows the mechanism of the process in addition to the possibility of improving the efficiency of some modification for algae, as well as conducting the process in an open system.

List of abbreviations

	Fourier Transmission Infra Red
	FTIR

	Thermal gravimetric analysis
	TGA

	Revolution per minute
	rpm

	Atomic Absorption Spectrophotometer
	AAS

	Deionized distilled water
	DDW

	Acidity Scale
	pH


Declarations
Ethics approval and consent to participate

Not applicable
Consent for publication

Not applicable
Availability of data and material

The datasets used and/or analyzed during the current study are available from the corresponding author on reasonable request.

Competing interests

The authors declare that they have no competing interests
Funding

Not applicable
Authors' contributions

All authors read and approved the final manuscript
Acknowledgments
Authors are thankful to the Department of Chemical Engineering labs, College of Engineering, University of Diyala, Diyala, Iraq, for financial support.
References

[1] Ghaedi, M.,. (2006) " Pyrimidine-2-thiol as selective and sensitive ligand for  preconcentration and determination of Pb2+". Chem. Anal 51, 593–602. 

[2] Hawari, A.H., Mulligan, C.N., (2006) "Heavy metals uptake mechanisms in a fixed bed column by calcium treated anaerobic biomass". Process Biochem. 41, 187–198.     
[3] S.P.K. Sternberg, R.W. Dorn, (2002) "Cadmium removal using Cladophora in batch, semi-batch and ﬂow reactors." Biores. Technol. 81 (3) 249–255.

[4] A. Kapoor, T. Viraraghavan, D.R. Cullimore, (1999)  "Removal of heavy metals using fungus Aspergillus niger."  Biores. Technol. 70 (1) 95–104.

[5] Selatnia, A., et al., "Biosorption of lead(II) from aqueous solution by a bacterial dead Streptomyces rimosus biomass." Biochem. Eng.J. (2004) 19,127–135.

[6] McKay, G.; Ho, Y. S.; Ng, J. C. P (1999) " Biosorption of copper from waste waters: a review."  Sep. Purif. Methods, 2, 87–125.
[7] Dambies, L.; Guimon, C.; Yiacoumi, S.; Guibal, E. .(2001) "Characterization of metal ion interactions with chitosan by X-ray photoelectron spectroscopy." Colloid Surf., A 17, 203–214.

[8] Figueira, M. M.; Volesky, B.; Mathieu, H. J. .(1999) " Instrumental analysis study of iron species biosorption by Sargassum biomass." Environ. Sci. Technol 33, 1840–1846.

[9]  Buschmann, J.; Sigg, L. (2004) " Antimony(III) binding to humic substances: Influence of pH and type of humic acid". Environ. Sci.Technol. 38, 4535–4541.
 [10] Salah N. Farhan,” Biosorption of Hg and Ni ions on Bakers Yeast” Diyala Journal  of Pure Science, Vol. 6 Issue 1, pages (2010) 157-173

[11] Loutseti S. ,et.al. (2009) "The application of a micro-algal/bacterial bioﬁlter for the detoxiﬁcationof copper and cadmium metal wastes.” Bioresource Technology 100 2099–2105.

[12] Shukla, A., et al. (2002) "The Role of Sawdust in the Removal of Unwanted Materials from Water." Journal of Hazardous Materials. B95. pp. 137-152.

[13] Pappalardo,  L.,  Jumean,  F.  and  Abdo,  N. ( 2010). " Removal  of  Cadmium,  Copper,  Lead  and  Nickel  from  Aqueous Solution by White, Yellow and Red United Arab Emirates Sand." American Journal of Environmental Sciences. 6(1): pp 41-44.

[14] Kumar,  U. (2006)"Agricultural  Products  and  By-products  As  a  Low-cost  Adsorbent  for  Heavy  Metal  Removal  from Water and Wastewater: A Review." Scientific Research and Essay. 1(2): pp 033-037. 

[15] Oboh, I., Aluyor, E. and Audu, T. (2009) "Biosorption of heavy meatls ions from Aqueous Solutions Using a Biomaterial." Leonardo Journal of Sciences. 14. pp: 58-65.

[16]  V.K. Guptaa,b , Bina Guptaa, Arshi Rastogic, Shilpi Agarwald, Arunima Nayaka (2011) "A comparative investigation on adsorption performances of mesoporous activated carbon prepared from waste rubber tire and activated carbon for a hazardous azo dye—Acid Blue 113"  Journal of Hazardous Materials 186 891–901

[17] Wael M. Ibrahim , Asad F. Hassan , Yahia A. Azab  (2016) "Biosorption of toxic heavy metals from aqueous

solution by Ulva Lactuca activated carbon" Egyptian journal of  basic and applied science 3 241–249.

[18] Veglio F.,  Beolchini F. (1997) " Removal of metals by biosorption: a review." Hydrometallurgy  44  301–316.

[19] A.I. Ferraz, T. Tavares, J.A. Teixeira, (2004) " Cr(III) removal and recovery from Saccharomyces cerevisiae."  Chem. Eng. J. 105 11–20.

[20] D.P.Mungasavalli, T. Viraraghavan, Y. Chung Jin, " (2007) Biosorption of chromium from aqueous solutions by pretreated Aspergillus niger: batch and column studies."Colloids Surfaces A: Physicochem. Eng. Aspects 301 214–223.

[21] Kanamadi, R.D., Ahalya, N. and Ramachandra, T.V. -(2006) "Biosorption of heavy metals  by Low-Cost Adsorbents." CES Technical Report112. Energy and Wetlands Research Group.

[22] Gardea-Torresdey,  J.L,  De  la  Rosa,  G.  and  Peralta-Videa,  J.R. .(2004 )"Use  of  Phytofiltration  Technologies  in  the Removal of Heavy Metals: A Review". Pure and Applied Chemistry76(4), pp. 801–813.
[23] Hassan AF, Youssef AM.( 2014) "Preparation and characterization of

microporous NaOH-activated carbons from hydrofluoric acid

leached rice husk and its application for lead(II) adsorption.

Carbon Lett;15(1):57–67.

[24] Hui TS, Zaini MAA.( 2015" Potassium hydroxide activation of activated carbon: a commentary. Carbon Lett; 16(4):275–

80.

[25] Salah N. Farhan, Anees A. Khadom (2015)” Biosorption of heavy metals from aqueous solutions by Saccharomyces Cerevisiae.” Int J Ind Chem 6:119–130 

[26] Sud, D, Mahajan, G. and Kaur, M.P. (2008) " Agricultural Waste Material as Potential Adsorbent for Sequestering Heavy Metal Ions from Aqueous Solutions – A Review." Bioresource Technology 99(14): pp 6017-6027. 
[27] Bunluesin, S., et al. (2007)  " Batch and Continuous Packed Column Studies of Cadmium Biosorption by Hydrilla verticillata." Journal of Bioscience and Bioengineering 103 (6), 509–513 

[28] Zhang, L.; et al. (2008) " Analysis of Infrared Spectrum of native wheat straw." Spectrosc. Spect. Anal. 28 (suppl.), 45–46.

[229]  A. Mittal, L. Kurup, J. Mittal, "Freundlich and Langmuir adsorption isotherms and kinetics for the removal of Tartrazine from aqueous solutions using hen feathers." J. Hazar. Mater. (2007) 146 243–248

[30] G.M. Gadd, L. De Rome(1988)." Microbial treatment of metal pollution: a working biotechnology." Appl. Microbiol. Biotechnol.610 [31] B. Volesky. .(1990)" Biosorption of Heavy Metals."  CRC Press, Boca Raton, FL.
Figures Title and Legend

[image: image4.png]Effect of temperature on

O pb with algae ashes

% Cuwith algae ashes

biosorption

—©— pb with algae

A Cuwith algae
16
14
12
w 10

)
£ 8
T 6
4
2
0
0 20 40

Temperature, C

80



[image: image3.png]T%

65

60

55

50

a5

40

Alcohol C:rbox\:l FTIR Mrethylen JHvdroxylsAmin

500 1500 2000 2500 3000 3500 4000
wave length

4500




Fig 1. FTIR spectra of algal biomass Chara Alge. Native                  Fig.3 Metal uptake, for lead and copper at different pH

[image: image5.png]Metal uptake vs Algae dose

~© pb(qg)Algae O gpbalaeash
& Cu(g)Algae % Cu(q)ash Algae

06



and treated with ions.
[image: image6.png]weight loss %

120

100

80

60

40

20

TGA

—0— Algae ashes O Algae

DD‘°*<> 000 o
o

oo
Ooo

200 400 600 800
Temperature, C

1000



                                                   

Fig 2. TGA for algae and algae ashes.
                           Fig. 4 Temperature Effect on metal ion biosorption.

[image: image7.png]Metal uptake,q, vs Time

~o-pb(gAlgee O qpbalae ash

A Cu(a)Algae 3 Cu(q) ash Algae
18
ooooooo
14 o

12 £ _
DOOWOOOOOO

o N & o ®

o

50 100 150 200
Time, min.




[image: image8.png]q, me/g

Lead (q), vs time at different
initial concentration

~o pb(a)Algae O qpbalae ash
A Cu(g)Algae % Cu(q)ashAlgae

9
s XXX KX XXX
;s i aaassbda
6
° goooan
4 o
oo

3 o
5 o

°
1
0

0 20 40 60 80

time, min

100




Fig.5 Metal uptake with increasing Bio adsorbent dose                   Fig. 6 Metal uptake,q, at varied time.
[image: image9.png]Metal uptake, q (mg/g) at
different pH

o pb(q)Algae O pb(q) algae ash
& Cu(g)Algae % Cu(q)algae ash

12

10





Fig. 7 Metal uptake for Lead with time at a varied initial concentration 

1

_1598076268.unknown

_1599041051.unknown

